## Slide 1: Micro Combustion Calorimetry & Milligram-scale Flame Calorimetry
Fernando Raffan
Lab Methods Day

## Slide 2: Flame Retardants
Brominated flame retardants (BFRs) are widespread in their use due to their relative low cost/high performance
Recently, BFRs have been found to accumulate in human tissues and persist in the environment1,2. Industry is moving towards suitable replacements
Understanding mechanisms of BFRs as gas phase combustion inhibitors can guide the research community towards a suitable replacement
A small scale screening tool for BFR replacements is highly desirable as it will considerably drive down costs during product development
1. http://www.epa.gov/oppt/existingchemicals/pubs/actionplans/pbde.html
2. http://www.nist.gov/el/fire_research/upload/1-Axelrad.pdf
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 3: UL-94
Qualitative test only
Sample is ignited, source is removed
Check for extinction and dripping
Rating

## Slide 4: Cone Calorimeter
  Commonly used in fire testing
  Controlled incident heat flux
  Requires samples on the order of grams (expensive for new materials)
  Laminar-Transitional Diffusion flames
  Incomplete combustion

## Slide 5: General Objectives
Scale down sample size, yet obtain meaningful results
Determine heat release rates and total heats of combustion of materials using mg sized samples
Use this information to characterize material flammability
Explore the effect of FR additives on performance
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 6: O2 Consumption Calorimetry
Huggett’s empirical observation: for most fuels, a nearly constant net amount of heat is released per unit mass of oxygen consumed for combustion.
  E = 13.1 + 0.6 kJ/g-O2

## Slide 7: O2 consumption calorimetry

## Slide 8: MCC
Objective
Measure heat release rate and total heat release of pyrolyzable materials (polymers) using mg sized samples
Approach
Uncouple pyrolysis from combustion
Premix volatiles with O2
High temperature furnace (900 C)
Long residence time (complete combustion)

## Slide 9: MCC Diagram
N2 inlet
Pyrolizer coil
Furnace coil
Sample
O2 inlet
Drierite
Flow Meter
O2 sensor

## Slide 11: MCC Calibration
Dedicated VI
  Run test with known metallic samples
  Compares measured temperature profile during pyrolyzer heating to known melting point of metal sample
  Compensates for difference
  Creates calibration file
Calibrating flow meters and O2 sensor
  Connect a reference flowmeter in series. Calibrate reference vs. MCC flow meter readout
  Purge furnace and flow N2 only. Record O2 sensor voltage.
  Purge furnace and flow calibration air (known O2 concentration). Record sensor voltage
  Apply linear relationship [O2]=mV+b

## Slide 12: MCC Operation
Sample preparation steps
  Cut/grind polymer to sub-mg pieces
  Condition in low humidity chamber
  Carefully weigh sample < 4 mg
Instrument preparation
  Open gas bottles and verify flowrates
  Start furnace
  Change setpoints if needed (default, no changes required)
Run Test
  Load sample carefully on pedestal
  Activate piston. Wait for flow rates to stabilize.
  Start process
  Data output (all flow rates, pyrolyzer T, HRR)

## Slide 13: MCC Operation

## Slide 14: MCC Data Analysis

## Slide 15: Data analysis
Run data analyzer
  Trim data endpoints
  Calculate total heat release
  Calculate derived quantities
FR sensitivity
  MCC does not detect FR effect on combustion efficiency
  Only effect of composition on heat release is detected
  Useful to determine HRR and total heat of combustion
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 16: MFC
Objective
Design and implement an apparatus that can study the flaming combustion of milligram scale solid samples in a well-controlled fashion
Correlate the measured gas-phase combustion efficiency with MCC and cone calorimetry results
Develop steps towards measurement of flame temperatures in polymers with/without flame retardants
The MFC
Milligram-scale Flame Calorimeter

## Slide 17: Design and Capabilities
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 18: Pyrolyzer
Purge gas
CDS 5000
Pyro-probe
Quartz tube
Sample tube

## Slide 19: Base
Insert coflow and igniter hardware
Homogenize coflow
Seal assembly

## Slide 20: Combustion Chamber
Enclose combustion process
Provide optical access to the flame for gaining information like flame height, flame structure, combustion time

## Slide 21: Gas Analyzing System
Drierite
Flow meter
O2 sensor
Hood
Pressure gauge
Soot filter

## Slide 22: Capabilities
Co-flow | 0 - 6.32 SLPM
O2 % in co-flow | 0-100%
Purge gas | 0-100 SCCM
Heating rate | 0-32 K/s
Co-flow | 4 SLPM
O2 inlet concentration | 20-21% (Air)
Heating rate | 10 K/s
Purge gas (N2) | 100 SCCM
Operating Conditions | 

## Slide 23: Repeatability
5 PMMA Tests

## Slide 24: Calibration
Similar to MCC (share same flow controllers/meters and O2 sensor type)
Pyrolyzer temperature profile determined with thermocouple embedded into ceramic filled sample tube (timeT)
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 25: Operation
Condition and prepare samples (~30 mg)
Replace soot filter
Open gas bottles. Activate flow controllers to desired setpoint
Load sample tube
Close system. Verify flowrate and O2 signals
Run pyroprobe and DAQ
Output: Time, O2 concentration, outlet flow rate
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 26: Operation
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 27: Flame Destabilization
Baseline PBT (no flame retardant)

## Slide 28: Flame Destabilization
55% PBT, 20% Al-DEP

## Slide 29: Data Analysis
Matlab code
  Read in files
  Process data using 2 methods (MFC and MCC)
  MCC method
  Customizable output (HRR curves, total HR)
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 30: MCC and MFC HRR
,⁰C
MCC
MFC

## Slide 31: Combustion Efficiency
Stoichiometry or MCC data

## Slide 32: CO Yields
For PS-FR2 ( 27.4 wt.% Br)
Gas phase combustion incompleteness:
43%
Formation of soot
Formation of CO and/or other incomplete combustion products
32%
11%
CO. yld (wt.%): 39.3%

## Slide 33: Conclusions
There are currently 2 experimental techniques to measure heats of combustion using mg-sized samples, MCC and MFC
MCC  smallest sample size, total heat of combustion, not sensitive to FRs, no soot produced
MFC flaming combustion, sensitive to FRs, soot and char yields can be measured, optical thermometry can be applied
Introduction
Flame Retardants
Current Test Methods
General Objectives
O2 Consumption Calorimetry
MCC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
MFC
Objectives and Approach
Apparatus Description
Calibration
Operation
Data Analysis
Derived Data
MCC and MFC HRR
Combustion Efficiency
CO yields
Conclusions

## Slide 34: Bibliography
Lyon, R. et al., “A Microcombustion Calorimeter,” DOT/FAA/AR-01/117 Report http://www.tc.faa.gov/its/worldpac/techrpt/ar01-117.pdf
Ding, Xi, “Design and Implementation of the Flaming Combustion Calorimeter,” M.S. Thesis, University of Maryland, 2013